Specification For Paddlewheel Flow Sensor

- Sensor shall be FM Class I (Group A, B, C, D), II (Group E,F,G), III, Division 1 (Groups A-G).

- The paddlewheel sensor shall be capable of pressures up to 103 bar (1500 psi) @ temperatures of 149°C (300°F).

- The paddlewheel insertion flow sensor shall generate an electrical signal proportional flow velocity from a range of 1.6 - 20 feet per second.

- The sensor shall be inserted at the correct depth and there shall be a fully developed flow profile.  Linearity of the output signal shall be ±1% of full range, with a repeatability of ±0.5% of full range.

- The sensor shall not create a pressure drop of >1 psi at any flow rate.

- Two optional sensor lengths shall allow the flow sensor to install into a flow installation fitting.  Optional sensor lengths will allow insertion in pipes from 0.5 to 12 inches.

- The sensor body materials shall be 316SS (ACI type CF-8M per ASTM A351), DIN 17440316SS (ACI type CF-8M per ASTM A351),DIN 17440, rotor material CB7Cu-1 Alloy rotor pin Tungsten Carbide GRP 1 (standard),or Stainless Steel (optional), (2): 316 stainless steel (1.4401) retainers, and with 2 rotor bearings made of Fluoroloy B®/PTFE

- The flow sensor shall be a Georg Fischer Signet model 525-1, 525-2, or equal.